TECHNICAL SPECIFICATION

FKM-Coupling RESISTOR

FKM-Coupling RESISTOR used in above ground chemical resistant plain ended industrial pipe systems with same diameters. The FKM-gasket allows a high chemical resistance and a thermal stability of up to +180°C.

Pipe 1 				DN/Material __________________

Pipe 2 				DN/Material __________________

Article Number 			__________________

____ Qty ____ Price/Unit ____ Total

Manufacturer:	MÜCHER DICHTUNGEN, D-50226 Frechen, T +49 2234 928 03-0, F -55

Pressure Tightness:		0.6 bar water / - 0.3 bar Vacuum

Jetting Resistance:		120 bar

Sealing Material:		FKM Fluororubber according to DIN ISO 1629

Stainless Steel:			AISI 304/1.4301 according to DIN EN 10088-2

Temperature Resistance:	-20°C to +180°C

Standard/Approval:		DIN EN 1629, CE18