TECHNICAL SPECIFICATION

Multi-Connector TRANSFER

Multi-Connector TRANSFER for the connection of plain ended industrial pipe systems from different materials with same or different diameters.

Pipe 1 				DN/Material __________________

Pipe 2 				DN/Material __________________

Article Number 			__________________

____ Qty ____ Price/Unit ____ Total

Manufacturer:	MÜCHER DICHTUNGEN, D-50226 Frechen, T +49 2234 928 03-0, F -55

Pressure Tightness:		0.6 bar water / - 0.3 bar Vacuum

Jetting Resistance:		120 bar

Sealing Material:		EPDM rubber according to DIN EN 681-1

Stainless Steel:			AISI 304/1.4301 according to DIN EN 10088-2

Temperature Resistance:	-40°C to +120°C, temporary max. temperature +160°C

Standard/Approval:		DIN EN 1629, CE18